## Slide 1
半导体刻蚀工艺良率分析报告
基于 10,000 条工艺数据的设备良率、交叉维度与关键影响因素分析
数据分析平台
2026.04 — 2028.07

## Slide 2
目录
01
执行摘要
全局良率概览与核心结论
02
数据概况
数据规模、字段分布与质量
03
设备良率对比
8台设备良率排名与时间趋势
04
交叉维度分析
设备×腔室、设备×配方、晶圆差异
05
关键影响因素
决策树特征重要性分析
06
聚类分析
K-Means 四簇工艺特征与风险分级
07
建议与行动项
优先级排序与预期收益
2/20

## Slide 3
01
执行摘要
全局良率 83.80%，设备间极差 4.65 个百分点
3/20

## Slide 4
核心指标一览
83.80%
全局平均良率
10,000 条记录，8 台设备，28 个月跨度
详细说明
最佳设备：ETCH08 — 86.55%
最差设备：ETCH01 — 81.90%
最佳组合：ETCH02×RECIPE_B — 89.34%
最差组合：ETCH05×CH4 — 78.37%
关键因素：厚度均匀性（44.7%）+ 缺陷密度（29.5%）
4/20

## Slide 5
02
数据概况
10,000 条记录 · 31 个字段 · 100% 完整度
5/20

## Slide 6
数据集基本信息
10,000
总记录数
31
字段数
100%
数据完整度
8
设备数
4
腔室数
6
配方数
25
晶圆数
28
月份跨度
6/20

## Slide 7
03
设备良率对比
ETCH08 领跑，ETCH01 持续下滑需重点关注
7/20

## Slide 8
各设备平均良率排名
排名
设备
平均良率
趋势
🥇
ETCH08
86.55%
➡️ 稳定
🥈
ETCH06
86.05%
➡️ 稳定
🥉
ETCH02
84.15%
➡️ 稳中有升
4
ETCH03
83.79%
➡️ 稳定
5
ETCH04
83.39%
⬆️ 后期改善
6
ETCH07
83.17%
⬇️ 后期下滑
7
ETCH05
81.91%
⬇️ 波动较大
8
ETCH01
81.90%
⬇️ 持续下降
8/20

## Slide 9
各设备月度良率趋势（2026.04 — 2028.07）
各设备月度良率趋势（2026.04 — 2028.07）
ETCH01
ETCH08
ETCH06
81
87
87
2026Q2
82
88
84
2026Q3
87
86
88
2026Q4
81
80
90
2027Q1
82
85
86
2027Q2
83
90
87
2027Q3
84
87
86
2027Q4
76
85
84
2028Q1
79
83
87
2028Q2
9/20

## Slide 10
04
交叉维度分析
设备×腔室、设备×配方、晶圆差异
10/20

## Slide 11
设备 × 腔室 良率
letter
col_title
points
letter
col_title
points
11/20

## Slide 12
设备 × 配方 良率
letter
col_title
points
letter
col_title
points
12/20

## Slide 13
晶圆良率分布 — 仅 Wafer 24 统计显著偏低
83.80%
全局均值
Wafer 24 — 79.27% (显著偏低) 4%
Wafer 08 — 81.39% 4%
Wafer 14/20 — 81.9~82.1% 8%
其余 21 片晶圆 — 82.5~86.6% 84%
13/20

## Slide 14
05
关键影响因素
决策树 C4.5 — 测试准确率 76.40%，AUC 0.652
14/20

## Slide 15
特征重要性排名
排名
特征
重要性
累计贡献
🥇
厚度均匀性 (thickness_uniformity_pct)
44.7%
44.7%
🥈
缺陷密度 (defect_density_per_cm2)
29.5%
74.2%
🥉
CF₄ 气体流量 (gas_CF4_sccm)
18.4%
92.6%
4
设备编号 (tool_id)
1.4%
94.0%
5
颗粒数 >0.5μm
0.8%
94.8%
15/20

## Slide 16
06
聚类分析
K-Means (K=4) — 识别出高风险工艺簇
16/20

## Slide 17
四簇工艺特征对比
簇
占比
厚度均匀性
缺陷密度
良率纯度
风险等级
C0
50.0%
2.02%
0.031/cm²
94.1%
✅ 优质
C1
25.3%
2.05%
0.037/cm²
93.9%
✅ 良好
C2
14.1%
2.08%
0.144/cm²
62.7%
⚠️ 风险
C3
10.5%
5.30%
0.044/cm²
61.2%
🔴 高风险
17/20

## Slide 18
07
建议与行动项
8 项行动，按优先级排序
18/20

## Slide 19
行动项清单
action_title
timeline
desc
负责人：owner
action_title
timeline
desc
负责人：owner
action_title
timeline
desc
负责人：owner
action_title
timeline
desc
负责人：owner
action_title
timeline
desc
负责人：owner
action_title
timeline
desc
负责人：owner
action_title
timeline
desc
负责人：owner
action_title
timeline
desc
负责人：owner
19/20

## Slide 20
谢谢
通过数据驱动决策，持续优化刻蚀工艺良率